| TECHNICAL DATA SHEET |  |  |  |  |
| --- | --- | --- | --- | --- |
| Trade Name | IRON OXIDE ORANGE |  |  |  |
| Type | 960 |  |  |  |
| REACH | Registration No.01-2119457614-35-0043,01-2119457554-33-0014 |  |  |  |
| Chemical Name | Synthetic iron oxide |  |  |  |
| Delivery form | Powder |  |  |  |
| CAS No. | 1309-37-1,20344-49-4/215-168-2,243-746-4 |  |  |  |
| Specifications | Contents(Fe2o3.aH20) | % | ≧88 | ISO1248 |
|  | Oil Absorption | ml/100g | 23-35 | ISO787-5 |
|  | Res.on 325 mesh | % | ≤0.3 | ISO787-7 |
|  | Water soluble salts | % | ≤0.3 | ISO787-3 |
|  | Moisture | % | ≤1.0 | ISO787-2 |
|  | PH value |  | 4-7 | ISO787-9 |
|  | Bulk Density | g/cm³ | 0.4-0.6 | ISO787-11 |
|  | Specific gravity | g/cm³ | 4.5 | ISO787-10 |
|  | Tinting Strength | % | 95～105 | ISO787-24 |
|  | Dispersibility(Hegman) | μm |  | ISO787-20 |
|  | Particle Size | μm |  |  |
|  | Color Difference △E |  | ≤1.0 | ISO787-1 |
| Sales Packing | In 25kg paper bag/1000kg bulk bag then palletized |  |  |  |

| Transport &Storage | Protect against weathering. Store in a dry place and avoid extreme fluctuations in temperature. Special conditions for opened packaging: close bags after use to prevent the absorption of moisture and contamination |
| --- | --- |

| Safety | The product is not classified as dangerous under the relevant EC directives and corresponding national regulations valid in the individual EU member states. It is not dangerous according to transport regulations. In countries outside the EU, compliance with the respective national legislation concerning the classification, packaging labeling and transport of dangerous substances must be ensured. The information contained in the safety data sheet should be observed. This contains informaiton on handingm product safety and ecology |
| --- | --- |

This information is given in good faith, without warranty. It is also applies where proprietary rights of third parties are involved. Our advice does not release you from the obligation to verity the information currently provided and to test our products as to their suitability for the intended processes and uses. The application, use and processing of our products and the products manufactured by you on the basis of our technical advice are beyond our control and, therefore, entirely your own responsibility. Our products are sold in accordance with the current version of our general conditions of sale and delivery.